[image: image1.png]@\
/ﬂfei?COﬂSf

IIIIIIIIIIIIIIIII




APPLICATION:
ROOFING

ASSEMBLY:

EXTENSIVE GARDEN ROOF 



W/FABRIC REINFORCED










MM 6125 (215 MILS)

EXTENSIVE GARDEN ROOF® ASSEMBLY

LONG FORM SPECIFICATION
PART I GENERAL

1.01
Summary
A.
This specification serves as a guideline and shall be adapted to suit the needs of each individual project by the architect.  It is prepared in accordance with the CSI three-part section format and shall be included as a separate section under DIVISION 7 - Thermal and Moisture Protection.  Improvements and other changes to the contents shall be made only with the written approval of the architect.

1.02
RELATED SECTIONS (Edit to project requirements)

A.
DIVISION 2 - Sitework [Section 02500/02870] - Paving/Site Furnishings as supplied by  Hydrotech, Membrane Corp.  See Division 7 for specific details.
B.
DIVISION 3 - Concrete [Section 03300] - Roof Deck Surface/Substrate

The coordination of this section is necessary to facilitate the successful installation of the waterproofing membrane.

Cast in Place Concrete/Composite Deck

A.
Strength/density:  
minimum  2,500 psi (17,235 kPa) compressive strength






minimum 115 pcf (1842 kg/m3) density

B.
Finish:


Wood-float or wood-troweled equivalent finish.  Steel




troweled is not desirable.

C.
Concrete Hydration (Cure):

1.
Method of Cure:  Water cure, wet coverings, paper sheets, plastic sheets or approved liquid curing compound (sodium silicate preferred).  Contact Hydrotech for other alter​na​tives.
2.
Duration of Cure/Dry:

a.
Structural Weight Concrete:  recommend 28 days, minimum 14 days, prior to application of the membrane.

b.
Lightweight Structural Concrete:  recommend 60 days, minimum 28 days, prior to application of membrane. Venting of the deck from the underside is recommended to facilitate drying.

c. The above minimum cure/dry times are recommended based upon basic concrete fundamentals and experience. Depending on conditions (i.e., ambient temperature, humidity) the concrete may be dry enough to receive application of the membrane in less than the 14 day minimum recommendation. Consult Hydrotech for specifics when less than the minimum is desired.


*REFER TO SECTION 3.02 PREPARATION FOR ADDITIONAL DECK TYPES.*
C. DIVISION  [ ] - Wood blocking and curbing

D. DIVISION  [ ] – Insulation

E. DIVISION  [ ] - Sheet metal flashing and counterflashing

F. DIVISION  [ ] - Prefabricated roof specialties

G. DIVISION  [ ] - Caulking and sealants

H. DIVISION  [ ] - Plumbing specialties

I. DIVISION  [ ] - Roof hatches

J. DIVISION  [ ] - Landscaping

1.03
REFERENCES
A.
American Society for Testing and Materials (ASTM).

B.
Canadian General Standards Board, CGSB-37.50-M89, Standard for Asphalt, Rubberized, Hot Applied, for Roofing and Water​proofing.

C.
Underwriters Laboratories (UL) Class A.

D. Dow Chemical Company, TechNote 508 Ballast Design Guide for IRMA Roofs.

1.04 DEFINITIONS

A.
Green Roof -- An area of planting/landscaping, built up on a waterproofed substrate at any level that is separated from the natural ground by a man-made structure.

B.
Extensive Green Roof -- Low to no maintenance landscaping consisting of shallow soil depths (< 6 inches (152mm) with plant varieties restricted to primarily mosses, herbs and succulents capable of withstanding harsh growing conditions.

C. Intensive Green Roof -- Landscaping requiring regular maintenance, consisting of deeper soil depths (> 8 inches (203mm) with a wider variety of plant species possible including shrubs and small trees.

D. Shallow-Intensive/Lawn Green Roof -- Landscaping requiring more regular maintenance than an extensive condition but limited in plant selection due to shallower soil depths, (i.e., sod grass lawn). 

E.
Garden Roof® -- Patented system of drainage, water retention and root barrier components utilized in the construction of green roofs over Hydrotech's MM 6125EV® roofing membrane.

F.
Steep Slope Green Roof -- Defined as a slope exceeding 3:12 pitch.
G. “C” Factor -- The runoff coefficient used in the Rational Method, “C” represents the portion of the storm rainfall that becomes runoff. 

H. Curve Number (CN) -- A number that is used with Natural Resource Conservation Service (SCS) methods to convert rainfall depth into runoff volume. The Curve Number takes into account a site’s soil type, plant cover, impervious cover, interception and surface storage. 
1.05
SYSTEM DESCRIPTION
A.
Furnish and install a completed Extensive Garden Roof® Assembly including roof substrate board (if required), surface conditioner (if required), Monolithic Membrane 6125EV®-FR and flashings, protection course, root barrier protection, STYROFOAM® brand insulation (if required), water retention mat (if required), drainage/water retention component, filter fabric, lightweight engineered growing medium (soil) and vegetation.
1.06
SUBMITTALS
A. Certification from an approved independent testing laboratory experienced in testing rubberized asphalt material, that the material meets the CGSB-37.50-M89 standard for rubberized asphalt membranes, including applicable ASTM procedures.

B.
Certification showing full time quality control of production facilities responsible for the manufacture of the rubberized asphalt and that each batch of material is tested to insure conformance with the manufacturers published physical properties.

C.
Certification showing that all components of the green roof assembly are being supplied and warranted by a single-source manufacturer.
D.
Evidence that the roof membrane assembly is currently Class A listed with Underwriters Laboratories.

E.
Evidence that the extruded polystyrene insulation if used is free from CFC's.

F. The plant manufacturing the rubberized asphalt material shall have IS0 9001-2000 approval as evidenced by a notarized copy of the official certificate.

G. Provide product data on all components of the green roof assembly.

1.07
QUALITY ASSURANCE
A.
Refer to Section 1.05 SUBMITTALS.  Include items A., B., C. & D.

B.
The Roofing/Waterproofing Contractor shall demonstrate qualifica​tions to perform the work of this Section by submitting the following documentation:

1.
Certification or license by the membrane manufacturer as a locally based, authorized applicator of the product the installer intends to use, for a minimum of five (5) years.

2.
List of at least three (3) projects, satisfactorily completed within the past five (5) years, of similar scope and complexity to this project.  Previous experience submittal shall correspond to specific membrane system proposed for use by applicator.

C.
Refer to Section 1.04 SYSTEM DESCRIPTION.  Include single-source for all components from the manufacturer.

D.
The rubberized asphalt membrane product shall contain an inert clay filler and crumb rubber to enable the product to be resistant to acids (fertilizers, building washes and acid rain) and maintain membrane thickness during application.

E. Membrane Manufacturer shall have available an in-house technical staff to assist the contractor, when necessary, in application of the products and final inspection of the assembly.

F.
Membrane Manufacturer Qualifications:  Manufacturer shall demon​strate qualifications to supply materials of this section by certifying the following:

1.
Membrane Manufacturer shall show evidence that the specified rubberized asphalt has been manufactured by the same source for fifteen (15) years and successfully installed on a yearly basis for a minimum of fifteen (15) years on projects of similar scope and complexity.

2. Membrane Manufacturer shall not issue warranties for terms longer than they have been manufacturing their hot fluid rubberized asphalt membrane.

G. Green roof supplier shall provide data and calculations to verify that the green roof assembly meets the project criteria for storm water runoff volume and rate control. 

1.
Calculations shall be based on actual testing of suppliers’ green roof components to be used for the project including but not limited to the growing media formulation and water retention/drainage materials.
2.
Calculations shall account for vegetated and un-vegetated portions of the roof and local climatic conditions including rainfall depth, intensity, duration, and timing. 

H. Green roof supplier shall provide data demonstrating that the composite C-factor and Curve Number parameters for the specified green roof assembly are less than or equal to those factors used in the engineering design and analysis for the projects drainage and storm water systems analysis if required.
I.
Pre‑Construction Conferences.  The manufacturer will meet with the necessary parties at the jobsite to review and discuss project conditions as it relates to the integrity of the roofing assembly.

1.08
DELIVERY, STORAGE AND HANDLING
A.
Deliver materials in original unopened containers of packaging clearly labeled with manufacturer's name, brand name, instruction for use, all identifying numbers, and U.L. labels.
B.
Materials shall be stored in a neat, safe manner, not to exceed the allowable structural capacity of the storage area.

C.
Store materials in a clean, dry area protected from water and direct sunlight.

D.
Store all adhesives at temperatures between 60°F (15.5°C) and 80°F (26.6°C).  If exposed to lower temperatures, restore materials to 60°F (15.5°C) minimum temperature before using.
E. Keep roof substrate board dry before, during, and after installation. Outside storage shall be off ground and protected by a breathable waterproof covering. Roof substrate board shall be roofed the same day as installed. 

F. Roof substrate board shall be cut to size using a sharp utility knife and straightedge. The surface of the roof substrate board shall be scored with the utility knife and the board bent up sharply towards the score cut. A keyhole-type drywall saw shall be used for penetration cutouts and radii. A low rpm circular saw shall be used for 5/8 inch thick roof board. 

1.09
PROJECT CONDITIONS
A.
Application of the membrane shall not commence nor proceed during inclement weather.  All surfaces to receive the membrane shall be free of water, dew, frost, snow and ice.

B.
Application of membrane shall not commence nor proceed when the ambient temperature is below 0°F (-17.7°C).

C.
Preparation and application of membrane shall be conducted in well ventilated areas.

D.
Over its service life, do not expose membrane or accessories to a constant temperature in excess of 180°F (82°C) (i.e., hot pipes and vents or direct steam venting, etc.).

E.
Adhesives contain petroleum distillates and are extremely flam​mable.  Do not breathe vapors or use near an open fire.  Do not use in confined areas without adequate ventilation.  Consult container or packaging labels and Material Safety Data Sheets (MSDS) for specific safety information.
F.
Do not allow waste products (petroleum, grease, oil, solvents, vegetable or mineral oil, animal fat, etc.) to come in contact with the roof membrane.  Any exposure to foreign materials or chemical discharges shall be presented to membrane manufacturer for evalua​tion to determine any impact on the roof membrane assembly performance.

G.
Concrete Deck Surface Condition.  IMPORTANT ‑ Refer to 1.02 Related Sections.
H. Deck Preparation; refer to Section 3.02 Preparation.

I. Deck slopes greater than 3 inches in 12 inches (approx. 15 degrees or 25%) shall be limited to extensive and shallow-intensive applications and require special installation considerations.  CONTACT Hydrotech for specifics.
J. Roof substrate board edges and ends shall be butt loosely in typical installations. Long, uninterrupted runs (greater than 200 feet) of roof substrate board may require slight gapping due to higher temperature gain. Gapping shall not exceed 3/16 inch and all such gaps shall be filled flush with the surface of the roof board with an appropriate sealant. CONTACT Hydrotech for specifics.
K. Humidity and temperature conditions, building location, building use and occupancy conditions may require the installation of a vapor retarder underneath roof substrate boards to prevent moisture condensation within the roofing assembly. The decision to use a vapor retarding membrane is the responsibility of the design professional.
L. Ballasting requirements vary depending on height of roof deck, parapet height, and design wind speed based upon location of building.  Vegetated green roofs also require proper ballasting and the possible use of wind erosion mats.  Ballast design shall be in accordance with Dow Chemical Company Technote 508 Ballast Design Guide for IRMA Roofs, and other applicable codes or wind design guides. CONTACT Hydrotech for ballasting recommendations.
M. General Contractor shall assure that adequate protection is provided after installation so other trades do not damage membrane.

1.10
WARRANTY
A.
Upon completion of the work, the contractor shall supply the owner with a single-source warranty of Canadian  origin direct from the manufacturer.


Each warranty varies in scope and terms.  Contractor Warranty Program
            (Contact Hydrotech for exact terms and conditions to meet warranty requirements       Accredited including list of accredited contractors who qualify for program).
C.
Warranties available from the manufacturer: (Edit to project requirements)
1.
Material Warranty; excludes labor.

Duration:  2-, 5-, 10-, 15-, 20-year
2.
Watertightness Warranty; includes labor and material to maintain watertight condition and replacement of Hydrotech supplied roof substrate board.

Duration:  5-, 10-, 15-, 20-year
3.
Thermal Warranties; includes 80% retention of the original thermal value and remain on the deck at 70 mph wind gust.  Duration 5-, 10-, 15-, 20-year
4.
Total System Warranties; covers components of the green roof assembly, including membrane, flashing, insulation, Garden Roof® components, vegetation and pavers. Includes removal and replacement of the Garden Roof® components, vegetation, pavers and soil (≤24 inches deep) when supplied by and installed per Hydrotech's requirements and replacement of Hydrotech supplied roof substrate board.
A.
Duration of Membrane/Flashing:  5-, 10-, 15-, 20-year

(watertight condition)

B.
Duration of Insulation:  5-, 10-, 15-, 20-year

(80% of original thermal value; remain on the deck withstanding wind speeds not to exceed 70 mph)

C. Material Integrity of Garden Roof® Components:  5-, 10-, 15-year

D. Extensive Vegetation: 2-year thrive and coverage 


(plugs: min. 50% coverage end of year 1; 80% coverage end of year 2)

(sedum carpet: min. 75% coverage at delivery and end of year 1; 90% coverage end of year 2)
E.
Duration of Pavers: 5-, 10-year

(will not crack, split or disintegrate due to freeze-thaw)

**CONTACT HYDROTECH FOR EXACT WARRANTY TERMS AND CONDITIONS.**
PART II PRODUCTS

2.01
GENERAL
A.
Refer to Section 1.04, System Description.  All components shall be obtained as a single-source from the membrane manufacturer to ensure total system compatibility and integrity.


Manufacturer:

Hydrotech Membrane Corp.





10951 Parkway




Ville d”Anjou, Quebec H1J 1S1




800 361 8924 or 514 353 6000




FAX:  514 354 6649




Web Site:  www.hydrotechusa.com
          Regional representative; InterCoast Building Solutions Inc.

                                                    604-593-5601

2.02
MATERIALS
A.
Membrane

1.
Membrane shall be a hot, fluid applied, rubberized asphalt membrane meeting the CGSB-37.50-M89 standard and other pertinent physical properties:
· American Hydrotech, Inc., Monolithic Membrane 6125EV® (up to 25% post-consumer recycled-content)
	PROPERTY
	TEST METHOD
	TYPICAL RESULT

	Flash point
	ASTM D-92 

CGSB-37.50-M89
	<500°F*

(260°C)

	Penetration
	ASTM D-5329

CGSB-37.50-M89
	98 mm @77°F (25°C)

187 mm @122°F (50°C)

	Flow
	ASTM D-5329

CGSB-37.50-M89
	1.0 mm @ 140°F (60°C)

	Toughness


	CGSB-37.50-M89
	16.0 Joules

	Ratio of Toughness to Peak Load


	CGSB-37.50-M89
	0.069

	Water Vapor Permeability
	ASTM E-96, PROCEDURE E 

CGSB-37.50-M89
	0.3 ng/Pa(s)M2

	Water Absorption


	CGSB-37.50-M89
	.11 gram weight gain

	Low Temperature Flexibility

(-25°C)
	CGSB-37.50-M89
	No delamination, adhesion loss, or cracking

	Low Temperature Crack Bridging Capability


	CGSB-37.50-M89
	No cracking, adhesion loss, or splitting

	Heat Stability
	CGSB-37.50-M89
	No change in viscosity, penetra​tion, flow or low temperature flexibility

	Viscosity
	CGSB-37.50-M89
	11.0 seconds

	Water Resistance (5 days/50°C)
	CGSB-37.50-M89
	No delamination, blistering, emulsification, or deterioration

	Softening Point
	ASTM D-36
	180°F (82°C)

	Elongation
	ASTM D-5329
	1000% minimum

	Resiliency
	ASTM D-5329
	40% minimum

	Bond to Concrete
	ASTM D-5329
	Pass

0°F (-18°C)

	Acid Resistance
	ASTM D-896

Procedure 7.1 (N-8)
	Pass‑50% Nitric Acid

       ‑50% Sulfuric Acid

	Resistance to Hydrostatic Pressure
	ASTM D-08.22

Draft 2
(developed: D5385)
	100 psi

(equals 231 foot of head water)

	Resistance to Salt Water
	ASTM D-896 similar 20% sodium chloride sodium carbonate calcium chloride
	No delamination, blistering, emulsification or deterioration

	Resistance to Fertilizer
	ASTM D-896 similar undiluted, 15/5/5, nitrogen/phosphorus/potash
	No delamination, blistering, emulsification or deterioration

	Resistance to Animal Waste
	3-year exposure
	No deterioration

	Solids Content
	
	100%-no solvents

	Shelf Life
	
	10 years (sealed)

	Specific Gravity
	
	1.23 + .02

	*102°F more than the application temperature recommended by the manufacturer.


B. Roof Substrate Board (if required) (Edit to project requirements)

1.
Impact resistant, nonstructural, fiber-reinforced, gypsum panels made from 95% recycled content.

- Securock Gypsum-Fiber Roof Board as marketed by Hydrotech Membrane Corp. 

a. Miscellaneous

1. Fasteners and Plates

- Provide size and type in accordance with Factory Mutual and/or

applicable codes and to maintain structural integrity. Only 3 inch round

metal plates shall be used.
2. Adhesive

- Provide adhesive compatible with roof substrate board and insulation to

comply with Factory Mutual and/or applicable codes and to maintain

structural integrity.

3. Vapor Barrier

- Provide suitable vapor retarder as required by design professional.

2.
Other approved fire rated type "X" gypsum roof substrate board.

C. Surface Conditioner

1.
Asphaltic surface conditioner for concrete surfaces only
- Hydrotech, Inc., 56170 Surface Conditioner or Quick-Set Surface Conditioner by Hydrotech Membrane Corp.
D. Reinforcing

1.
Spunbonded polyester fabric (standard duty) reinforcing sheet.

- Hydrotech Membrane Corp. Flex Flash® F

2.
60-mil (1.5 mm) thick, uncured neoprene (heavy duty) reinforcing sheet.

- Hydrotech Membrane Corp. Flex Flash® UN

E. Flashing (Edit to project requirements)

1.
60-mil (1.5 mm) thick, uncured neoprene sheet.

- Hydrotech Membrane Corp. Flex Flash® UN

2.
157-mil (4 mm) thick, torch-grade, modified asphalt, reinforced flashing membrane.

- Hydrotech Membrane Corp. Flex-Flash® MB

F. Adhesives/Sealant

1.
Contact adhesive to bond elastomeric flashing together.

- Hydrotech Membrane Corp,  Splicing Cement

2.
Contact adhesive to bond elastomeric flashing to an approved substrate.

- Hydrotech Membrane Corp. Bonding Adhesive

3.
Sealant to seal elastomeric flashing seam edge.

- Hydrotech Membrane Corp., Lap Sealant

G. Separation/Root Barrier Protection Course

1.
Combination of a fiberglass reinforced rubberized asphalt protection sheet and polyethylene root barrier.

- Hydrotech Membrane Corp Hydroflex® 30/Root Stop
H. Prefabricated Drainage Course (If required, consult Hydrotech)
1.
Composite drainage system consisting of a three-dimensional, crush-proof, drainage core and a filter fabric.
- Hydrotech Membrane Corp. Hydrodrain® 300

I. Insulation (Edit to project requirements)

1.
Extruded polystyrene rigid board insulation for use above membrane.
- STYROFOAM® Brand insulation [TYPE] as manufactured by The Dow Chemical Company, marketed by Hydrotech Membrane Corp.

a.
Insulation shall meet CAN/ULC S 701 Type IV.
b.
Minimum compressive strength, ASTM D-1621, 35, 40, 60  or 100 psi (240, 276, 414 or 690 kPa) (variance by type of product)

c.
Maximum water absorption by volume per ASTM D 2842, 0.7%

d.
Water vapor permeance for 1" product per ASTM E-96, .6-.8 perm (max.) 35-45 ng/Pa/s/m2)

e.
Insulation shall have an R value of 5.0°F ft2 h/Btu/in. (0.88 K m2/W) of thickness when tested at 75°F (23.9°C) mean temperature in accordance with ASTM C-518 and C 177.
f.
Product shall be free of CFC's and HCFC’s.
Product types available:  STYROFOAM® Brand, Roofmate, HiLoad 40, HiLoad 60 and HiLoad 100. CONSULT Hydrotech for recommended product type.
J. Air Layer (If required, consult Hydrotech)

1.
Required air space over STYROFOAM® insulation when moisture mat is required shall be composed of a crush-proof core and non-woven filter fabric.

- Hydrotech Membrane Corp. Hydrodrain® AL or Hydrodrain 300. 
K. Water Retention Mat (If required, consult Hydrotech)

1. Non-woven, synthetic fiber mat capable of retaining additional moisture for potential use by vegetation.

- Hydrotech Membrane Corp. Moisture Mat

L. Drainage/Water Retention Component (Edit to project requirements)

1. Three-dimensional, molded panels of recycled polyethylene with drainage channels top and bottom sides and water retention reservoirs top side. 

- Hydrotech Membrane Corp.  Gardendrain®
a. Extensive Conditions:

· Gardendrain GR15 or Gardendrain GR30 
M      METAL EDGE RESTRAINT


.1
Product: metal edge restraint, dimensions to suit, fabricated of extruded  aluminium bent to a 90° angle, slotted  with 1.25 inch  slots to permit drainage.  Curve Rite 6X6 rigid with will finish.
.2
Product: connector piece, right angled or straight, fabricated of 2.54 mm thick aluminium, with openings to fasten retaining curbs one to each other.

M. Filter Fabric

1. Non-woven, polymeric, geotextile fabric.

-  Hydrotech Membrane Corp.  Systemfilter

N. Soil 

1. Custom growing media mix capable of supporting vigorous growth of the specified vegetation, complying with the following specification. 

- Hydrotech Membrane Corp. Extensive LiteTop® Growing Media 
	Property
	Extensive*
	
	

	Grain Size Distribution
	
	
	

	clay fraction
	< 1 %
	
	

	passing #200 sieve
	1-3 %
	
	

	passing #60 sieve
	5-25 %
	
	

	passing #18 sieve
	20-50 %
	
	

	passing 1/8-inch sieve
	55-95 %
	
	

	passing 3/8-inch sieve
	90-100 %
	
	

	Density
	
	
	

	Application Density
	0.6 - 1.1 g/cm3

(38 lbs – 69 lbs/cf)
	
	

	Saturated Density
	0.9 - 1.4 g/cm3

(56 lbs – 87 lbs/cf)
	
	

	Dry Density
	0.5 -1.0 g/cm3

(31 lbs – 62 lbs/cf)
	
	

	Water & Air Management (% vol.)
	
	
	

	saturated water capacity
	>30 %
	
	

	saturated air content
	>10 %
	
	

	Saturated Hydraulic Conductivity
	>0.6 mm/min

(>1.4 in/hr)
	
	

	pH, Lime, and Salt Content
	
	
	

	pH (saturated paste)
	6.0 - 7.5
	
	

	carbonate content
	<25 g/l
	
	

	salts content (water extract)
	<2.5 g/l

(<1.7 mmhos/cm)
	
	

	Organics
	
	
	

	OM content
	3 – 6 mass %
	
	

	C/N ratio
	<20
	
	

	Nutrients** (plant available)
	in lb/1,000 ft3
	
	

	nitrogen (NO3)
	3 – 15
	
	

	phosphorus
	1 – 7
	
	

	potassium
	6 – 15
	
	

	calcium
	19 – 65
	
	

	magnesium
	3 – 15
	
	

	CEC Capacity
	>5 cmol/kg
	
	


* Values shall be adjusted due to availability of local materials or special project conditions related to plant selection and/or environmental conditions.
** Nutrients shall be adjusted with appropriate slow-release fertilizer with micronutrient additions if below lower target range.
O. Vegetation/Plantings (Edit to project requirements, consult Hydrotech)

1.
 Hydrotech Membrane Corp Garden Roof Extensive PlantsTM


a.  
Vegetative Carpet

- Hydrotech Membrane Corp Garden Roof Extensive InstaGreen® Sedum Carpet
2.
Plugs, Sedum Cuttings, Sedum Carpet shall be planted and maintained in accordance with Hydrotech’s written specifications by an approved installer.
P. Hardscape / Roof Ballast (Edit to project requirements)

1.
Pavers

a.
Ballast Pavers

- Hydrotech Membrane Corp.  Ballast Pavers, meeting the following physical properties:

	PROPERTY
	TEST METHOD
	VALUES

	
	
	

	Compressive Strength
	ASTM C140
	>7,000 psi average min.

	Flexural Strength
	ASTM C293
	>600 psi average min.

	Water Absorption
	ASTM C140
	Not greater than 5%

	Freeze/Thaw
	ASTM C67
	<1% loss/dry weight (50 cycles)

	Centerload
	-
	Min. 1,750 lbs.


b.
Architectural Finish Pavers

- Hydrotech Membrane Corp.  Architectural Pavers, meeting the following physical properties:

	PROPERTY
	TEST METHOD
	VALUES

	
	
	

	Compressive Strength
	ASTM C140
	>7,000 psi average min.

	Flexural Strength
	ASTM C293
	>600 psi average min.

	Water Absorption
	ASTM C140
	Not greater than 5%

	Freeze/Thaw
	ASTM C67
	<1% loss/dry weight (50 Cycles)

	Centerload
	-
	Min. 1,750 lbs.


2.
Stone Ballast

Well screened and washed stone gravel meeting ASTM D-448-80, gradations #57, 2, 4 or 5 (as directed by Dow Chemical Company, TechNote 508 Ballast Design Guide for IRMA Roofs).

3.
Concrete Pour Topping

Note to specifier: Dow Chemical Company, manufacturers of STYROFOAM® Brand Insulation, recommends the incorporation of an air layer between the insulation and concrete.  Hydrotech suggests the use of Hydrodrain AL for this purpose.

2.03 RELATED MATERIALS
A. Metal counterflashing is typically required to provide protection to vulnerable flashing materials from damage due to gardening activities. 
PART III EXECUTION

3.01
INSPECTION
A.
The roofing contractor shall examine all surfaces to receive the roofing assembly to verify it is acceptable and proper for the application of the membrane.  Refer to Hydrotech's Pre-Installation & Application Guidelines.
B.
The roofing contractor shall not proceed with the installation of the roof membrane assembly until all roof defects have been corrected.

3.02
PREPARATION
A.
All surfaces shall be dry, smooth, free of depressions, voids, protrusions, clean and free of unapproved curing compounds, form release agents and other surface contaminants. (Edit to project requirements)
1.
Cast in-place concrete/Composite deck

a.
Poured in place concrete shall be monolithic, smooth, free of voids, spalled areas, laitance, honeycombs, and sharp protrusions.

b.
Refer to Section 1.02 of this specification, Division 3.
2.
Precast concrete decks

a. Precast units shall be mechanically secured to minimize differential movement and all joints between units shall be grouted.
3. Plywood decks

a. Minimum thickness of 1/2" (12.7 mm) is required with adequate structural support.

b. Tongue and groove joint edges are required.

c. Adequate number and type of fasteners shall be used to comply with applicable codes and maintain structural integrity.

4.
Metal Deck with roof substrate board (Edit to project requirements)

a.
Roof substrate board board shall be fire rated type "X" board attached to minimum 22 gauge steel decking with adequate structural support.

1. Minimum 5/8 inch thick substrate board shall be used directly to metal deck. 

2. Minimum 1/2 inch thick substrate board shall be used over insulation. 

b. Flat fill and sloped roof insulation shall be installed in accordance with layout indicated on shop drawings and insulation board manufacturer’s minimum requirements. 

c. Adequate number and type of fasteners shall be used to comply with roof substrate and insulation board manufacturer’s minimum requirements and applicable codes and to maintain structural integrity. 

1. A minimum of 10 fasteners per full-size roof board shall be used. 

d. Appropriate roof adhesive shall be used in accordance with adhesive manufacturer requirements to comply with applicable codes and maintain structural integrity.

1. Size and spacing of adhesive beads shall be as required by adhesive manufacturer.  

e. Roof substrate boards shall be installed such that all edge and end joints are supported by metal deck ribs and/or appropriate blocking.

f. Roof substrate board end joints of adjacent lengths shall be staggered. 

g. Where required, a suitable vapor barrier membrane shall be applied to the metal decking prior to installation of the roof substrate board. 

5. Re-Roof/Tear-Off Application

a. Asphalt, coal tar pitch or other existing membrane shall be removed.  CONTACT Hydrotech.

b. Deck type acceptable to Hydrotech.

B.
Substrate cleaning

1.
Thoroughly sweep the substrate which is to receive the roof membrane.

2.
Substrate shall also be blown clean using an air compressor to remove any remaining loose debris.
3.
Final check to determine if concrete has been properly cleaned is to apply a test patch of Monolithic Membrane 6125 to the surface and check its adhesion.

3.03
INSTALLATION
A.
Surface conditioner application (to concrete substrates only)

1.
Apply the surface conditioner only to concrete using a hand held sprayer evenly at a rate of 300 to 600 SF/gallon (7.4 - 14.7 m2/L) depending on surface texture.  Surface conditioner shall "tan" the surface, not blacken it.

2.
Allow sufficient time for the surface conditioner to thoroughly dry prior to the membrane application.

B.
Membrane preparation

1.
The membrane shall be heated in double jacketed, oil bath or hot air melter with mechanical agitation, specifically designed for the preparation of a rubberized asphalt membrane.

2.
Heat membrane until membrane can be drawn-free flowing at a temperature range between 350°F (176°C) and 375°F (190°C).

C.
Detailing/Flashing

1.
All detailing and flashing shall be done in accordance with the manufacturer's standard guideline details.

2.
All detailing and flashing shall be completed before installing the membrane over the field of the substrate.

3.
Roof substrate board joints shall be pre-detailed with membrane and fabric reinforcing prior to full fabric reinforced membrane application.

D.
Membrane Application

1.
Apply the rubberized asphalt membrane at a rate to provide a continuous, monolithic coat of 90 mil minimum (approximately 2.3 mm), into which is fully embedded a layer of the spunbonded polyester fabric reinforcing sheet, followed by another continuous monolithic coat of membrane at an average thickness of 125 mil (approx. 3.2 mm).  Total membrane thickness is to be 215 mils average (approx. 5.5 mm), 180 mils minimum.

2.
Overlap fabric reinforcing sheet 1-2 inches (25.4 mm - 50.8 mm) with membrane between sheets.

3. Pre-detailing of joints between plywood and roof substrate board decks is required.
3.04
SEPARATION/PROTECTION COURSE INSTALLATION
A.
Separation/Protection course shall be installed as follows: 

1. Embed the Hydroflex 30 separation/protection course into the membrane while it is still hot to insure a good bond. Installation of a separation course is necessary in order to carry out the water test.

a.      Overlap adjoining sheet edges (dry) a minimum of 2"-3" (50.8 mm - 76.2 mm)       to insure complete coverage.

3.05
GARDEN ROOF COMPONENTS INSTALLATION
A. Root Barrier Protection.  Root Stop shall be laid over the Hydroflex 30, lapping adjacent sheets 5 feet (1.5 m), or 1 foot (300 mm), overlap is acceptable if Seam Tape is used. The Root Stop shall be turned up all vertical, roofed/flashed surfaces to completely protect waterproofing and flashings. 

B. Insulation.  Where specified, STYROFOAM® brand insulation shall be installed loose-laid in accordance with manufacturer's recommendations.

C. Air Layer.  When insulation and Moisture Mat are specified an air layer shall be required between the surface of the insulation and the water retention mat. A layer of Hydrodrain AL or 300 shall be installed over the insulation. The 4 inch (100 mm) salvage edge of the geotextile fabric overlaps adjoining sheets and can be held in place with duct tape. 

D. Moisture Mat. Where specified, a layer of Moisture Mat shall be installed over the root barrier (when no insulation is specified) or air layer/ insulation, lapping adjacent rolls a minimum of 4 inches (100 mm). The Moisture Mat shall be turned up all vertical, roofed/flashed surfaces a minimum of 6 inches (150 mm) beyond the anticipated soil level. Any excess shall be trimmed down to the level of the soil.
E. Drainage/Water Retention Component. (Edit to project requirements)
1. Gardendrain GR15, Gardendrain GR30, shall be installed with holes through the dimples on top, over the root barrier protection, water retention mat (if used) or STYROFOAM® insulation (if used). Adjacent panels shall be butt together or overlapped approximately 1 inch (25 mm). Gardendrain shall be cut to fit around penetrations, etc. with a heavy-duty utility knife or small toothed saw.
2. METAL EDGE RESTRAINT INSTALLATION

.1
To ensure a continuous barrier between growing medium and vegetation free zone  strips, install retaining curbs directly onto the drainage/water retention panels where indicated.

.2
Abut and fasten retaining curbs one to the other using connector pieces.

F. Filter Fabric. (Edit to project requirements)
a. A layer of Systemfilter shall be laid over the Gardendrain, lapping adjacent rolls a minimum of 6 inches (150 mm). Enough material shall be left to be drawn up above the anticipated soil level. Any excess shall be trimmed down to the level of the soil.

b. For slopes ≥2:12 and <3:12 (approx. 10 - 15°, 17 - 25%) filter fabric shall not be installed over the Gardendrain GR30 (only) throughout the field of the roof so that the growing media shall be placed directly into the cups. Filter fabric shall be laid at penetrations, terminations, etc. 
3.06
HARD SCAPE/ACCESSORY INSTALLATION
A. Stone and/or paver ballast shall be installed at all roof perimeters, building walls, penetrations, and access hatches and as required for flashing vegetation barriers, proper wind design, fire breaks, and as walkway/maintenance paths. 

1.     Ballast design shall be in accordance with The Dow Chemical Company’s TechNote 508     Ballast Design Guide for IRMA Roofs, and other applicable codes or wind design guides.
B.
All drains shall be fitted with inspection/maintenance boxes and grills, built up to ensure access at soil level.

3.07
SOIL INSTALLATION  

A. LiteTop soil shall be placed carefully to avoid damage or displacement of other materials such as walls, paving, drainage components, filter fabric, and roofing membrane. 

B. LiteTop soil shall be placed to within 1 inch greater than final grade or to a depth of no greater than 8 inches and compacted as described in 3.08.C. below. For final grades less than 8 inches only one round of compaction shall be performed and remaining soil loosely placed such that top of soil exceeds final grade by 1 inch (see 3.08.D. below).  For final grades greater than 8 inches, place soil at no greater than 6 inches and repeat procedure until soil has been compacted within 1 inch of final grade. 
C. Compaction shall be performed with a 200 – 300 lb. landscape roller or lightly compacted with a hand held mechanical compactor to achieve a 50 – 60 % compaction as determined by ASTM D1557. 

D. After compaction remaining soil shall be placed at 1 inch greater than final grade and thoroughly watered or jetted over entire area. Low settled areas shall be filled with additional soil and re-wet to achieve uniform prescribed final grade.

E.
Erosion Control Mat.  (Edit to project requirements)

1.
The erosion control mat shall be installed directly over the growing media and properly staked into place.



a.    
Stake fastening pattern is based on local wind speed, building height and
                

roof slope.  Contact Hydrotech for specific guidelines.



b.        
Erosion control mat is not required when Sedum Carpet is installed; however the Sedum Carpet shall be staked in place as required.
3.08
VEGETATION INSTALLATION

A.
Vegetation planting and initial maintenance shall be in accordance with the Hydrotech                     Extensive Garden Roof Plants Installation and Maintenance Guideline. .1




.2  
All components of the garden roof system must be adequately installed prior to receiving sedum carpets to avoid trampling and storage of materials on the plants.


.3  
Planting shall be performed only between spring and fall, during plant growing season, and avoiding dry and intensely hot periods.  Do not plant when growing medium is frozen.


.4
Growing medium must be level (avoid localized depressions and footprints), compacted and completely saturated with water 24 hours prior to placing sedum carpets.


.5 
Ensure carpet roll’s growing medium is moist at time of delivery and correct if required with an oscillating sprinkler prior to hoisting onto roof. Store out of direct sunlight and keep rolls humid until unrolled.


.6 
If sedum carpets cannot be placed within one day of their delivery, they must be unrolled on plywood or cardboard in a cool and shady location.


.7 
Moisten an area of approximately 10 m2 where the first rolls of sedum carpet are placed to help alleviate stress on the root system.  Each roll must be placed on pre-moistened growing medium. Repeat process for every 10 m2 installation area.


.8  
Set the rolls down gently with the end (‘’the flap’’) on the bottom of the roll. Place this leading edge exactly and firmly against the starting edge. Unroll it, avoid moving the carpet due to the stress and tearing action this will have on the root system. Avoid exposing bottom of roll edges, if necessary, fold edges towards the interior.

.9 
From the starter roll, lay sedum carpet roll with staggered joints.  Joints between rolls shall touch but not overlap. Fill gaps over 25 mm with growing medium.  For gaps wider than 75 mm, patch with a piece of sedum carpet.

.10 When a 10 m2 area has been laid, commence watering this area for at least one hour using an oscillating sprinkler. Repeat the process for each following area of 10 m2.  At day’s end, the entire planted area must be watered until saturation of the carpet and growing medium’s components. 

3.09  MAINTENANCE DURING ESTABLISHMENT PERIOD

SPEC NOTE: Garden roof maintenance varies according to planting type.  Adapt following paragraphs to suit project’s specific requirements.

.1
Ensure maintenance of planted areas for a period of two (2) years.

.2
Perform maintenance described below between date of planting and date of acceptance by Architect.

.3
Inspect weekly for the first four weeks to take note of installation and maintenance defects and to correct such immediately.  Afterwards, inspections in late spring and early fall shall be performed as part of the scheduled two (2) year maintenance program.  Fill-out and submit appended maintenance control forms to garden roof system supplier for each inspection visit.

.4
Saturate growing medium during the critical establishment period, which is the first four weeks after planting; for the first week, water daily; second week, water every two days, third week, water every three days and, for the fourth week, water at least once during the week. A 25 mm rainfall replaces a watering.

.5
Planted areas and clean strips shall be kept clean of debris and dead plant matter.  If necessary, remove surplus of accumulated leaves and dead flowers and water profusely the plant material above ground and the growing medium if they are exposed to salt spray.

.6
Only in the case of plants suffering of important mineral deficiencies, uniformly spread a fertilizer or soil amendment after having informed the garden roof system supplier and the Owner. Spread half the required dosage in one direction, then spread the other half perpendicularly. A controlled release coated fertilizer such as Osmocote, Polyon or Nutryon is recommended every three years.

.7
During the first year, saturate the growing medium to avoid plant fading and water stress at all times.  Carefully watch prolonged dry spells where a considerable amount of water is required.  Except in emergency situations, avoid watering in full sunlight or hot temperatures as much as possible.
.8
During inspection visits, manually weed planted areas of all parts (aerial and roots) of all undesirable adventitious plants.  Weeding is much more frequent during the first year of establishment (at least four times) and diminishes the second year (at least twice) until complete coverage by the desired vegetation. In all cases, adventitious plants must be destroyed prior to their seeds maturing.

.9
At all times, unless indicated otherwise by the garden roof system supplier and the Owner, it is forbidden to use any pesticide (herbicide, fungicide, insecticide) or anti-parasitic product on the garden roof.

.10
Inspect and clean roof drains two to three times a year, especially at beginning and end of growing season.
.11
Replant areas where plants are dead or where areas are denuded after having informed the garden roof system supplier and the Owner, and this, until the end of warranty period.
3.10
ON-SITE QUALITY CONTROL
SPEC NOTE:  Inspection agency must be experienced in waterproofing membranes and their application. 

.1
Hot-applied rubberized asphalt membrane inspection and testing shall be carried out by an inspection agency selected by Architect [Consultant] [Engineer], in accordance with Section [01 45 00 – Quality Control].

3.20  ELECTRONIC MEMBRANE TESTING
.1
Electric membrane testing and quality control shall be performed using by Detec Membrane Integrity Testing and shall be paid by the Owner.

3.20
CLEANING
.1
Clean work area in accordance with Section [01 74 11 – Cleaning].

END OF SECTION

1
.11

copyright

